**Tender/document describing the selective demolition process in Guldborgsund Municipality.**

Yellow bricks inside and outside.

Exterior and interior bricks that are not painted can be used for recycling. Joints are generally easy to clean and should be recycled.

Demolition of bricks (bricks):

Bricks must be dismantled manually so that the bricks can be stacked in a pallet with side skirts (pallet frames) and transported to landfill according to the client's instructions. Bricks must be removed carefully and individually so that they can be reused. Bricks with chips, cracks or flaking must be separated and disposed of. Expect 20% of the brick to be disposed of

Bricks must be cleaned of mortar before stacking. This can be done by setting up elephant grids on trestles to scrape the bricks clean.

Bricks stacked in pallet frames are the property of the client. Pallets and pallet frames must be supplied for stacking all materials for recycling. Pallets and pallet frames are subsequently the property of the developer.